## Slide 2
Quartz crystal microbalance and lipid membranes

## Slide 3
Experiment
DPPC Tm 41.5 °C
Vesicles extruded with 100 nm pore membrane
Au-coated quartz
Effect of hydrophobic chain length on melting temperature?
DPPC is 16:0, we will measure 15:0, 17:0 and I’ll provide you with data for 14:0

## Slide 4
Step 1. Sensor cleaning
Task 1 to be included in the report: How does UV-ozone work?

## Slide 5
Step 2. Measure contact angle and calculate surface energy
Liquids: Water and diiodomethane
Task 2 to be included in the report: Calculate surface energy

## Slide 6
Step 3. Mount the QCM-D sensors in the QCM-D instrument

## Slide 7
DPPC lipid
(Tm ~ -17 °C)
Lipid film formation:
Evaporation of solvent (clorophorm)
Lipid film hydration
With HEPES buffer
Extrusion
How to form lipid vesicles?

## Slide 8
1) Dry lipid film
Step 4. Formation of vesicles
2) Overnight low pressure
3) Hydration
4) Vortexing

## Slide 9
Step 5. Extrusion

## Slide 10
Step 6. DLS and zeta potential measurement
We will not do it this time since the instrument is busy

## Slide 11
Vesicle adsorption process

## Slide 12
Vesicle adhesion
The shape of the adhered vesicle is determined by the interplay of adhesion and bending energies
A*
Afree
W. Helfrich, Z. Naturforsch. 28c,693 (1973).
R. Lipowsky and U. Seifert, Mol. Cryst. Liq. Cryst. 202, 17 (1991)
Curvature

## Slide 13
Vesicle adhesion
A*
Afree

## Slide 14
SiO2
Adhesion favours vesicle fusion
Strong adhesion
C.A. Keller, Biophys. J. 75, 1397 (1998)

## Slide 15
Au
Weak adhesion
No rupture, intact vesicle layer
C.A. Keller, Biophys. J. 75, 1397 (1998)

## Slide 16
Task 3 to be included in the report: Plot Δfn and ΔDn time dependence
and describe the adsorption process and layer formation

## Slide 17
Task 4 to be included in the report: Plot −ΔDn/Δfn vs −Δfn time dependence
and describe the adsorption process and layer formation
Compare the size obtained with pore size to extrude vesicles in bulk
E. Tellechea, Langmuir 25, 5177 (2009)

## Slide 18
Monitoring lipid bilayer phase transitions
Neupane et al. Frontiers in Materials 5, 1096 (2018)

## Slide 19
Analyzing the data

## Slide 20
Sensor number
Overtone number
The fundamental overtone is very unstable, start from the 3rd
Analyzing the data

## Slide 21
Overall experiment

## Slide 22
Overall experiment

## Slide 23
Initial adsorption

## Slide 24
Layer thickness estimation
Plot −ΔDn/Δfn vs −Δfn time dependence
E. Tellechea, Langmuir 25, 5177 (2009)